## Slide 1: Chapter 6 Photolithography
Prof.M.D.Shirsat

## Slide 2: Objectives
List the four components of the photoresist
Describe the difference between +PR and -PR
Describe a photolithography process sequence
List four alignment and exposure systems
Describe the wafer movement in a track-stepper integrated system.
Explain relationships of resolution and depth of focus to wavelength and numerical aperture.

## Slide 3: Introduction
Photolithography
Temporarily coat photoresist on wafer
Transfers designed pattern to photoresist
Most important process in IC fabrication
40 to 50% total wafer process time
Determines the minimum feature size

## Slide 4: Applications of Photolithography
Main application: IC patterning process
Other applications: Printed electronic board, nameplate, printer plate, and et al.

## Slide 5: IC Fabrication
e-Beam or Photo
EDA PR Chip
Photolithography
Ion Implant
Mask or Reticle
Etch
EDA: Electronic Design Automation
PR: Photoresist

## Slide 6: IC Processing Flow
Materials
IC Design
Masks
IC Fab
Test
Packaging
Final Test
Thermal Processes
Photo-lithography
Etch
PR strip
Implant PR strip
Metallization
CMP
Dielectric deposition
Wafers

## Slide 7: Photolithography Requirements
High Resolution
High PR Sensitivity
Precision Alignment
Precise Process Parameters Control
Low Defect Density

## Slide 8: Photoresist
Photo sensitive material
Temporarily coated on wafer surface
Transfer design image on it through exposure
Very similar to the photo sensitive coating on the film for camera

## Slide 9
Photoresist
Negative Photoresist
Becomes insoluble after exposure
When developed, the unexposed parts dissolved.
Cheaper
Positive Photoresist
Becomes soluble after exposure
When developed, the exposed parts dissolved
Better resolution

## Slide 10
Mask/reticle
Exposure
After Development
Negative Photoresist
UV light
Positive Photoresist
Substrate
Substrate
Substrate
Photoresist
Negative and Positive Photoresists
Substrate
Photoresist

## Slide 11: Photoresist Chemistry
Start with printed circuit
Adapted in 1950 in semiconductor industry
Critical to the patterning process
Negative and positive photoresist

## Slide 12: Photoresist Composition
Polymer
Solvents
Sensitizers
Additives

## Slide 13: Polymer
Solid organic material
Transfers designed pattern to wafer surface
Changes solubility due to photochemical reaction when exposed to UV light.
Positive PR: from insoluble to soluble
Negative PR: from soluble to insoluble

## Slide 14: Solvent
Dissolves polymers into liquid
Allow application of thin PR layers by spinning.

## Slide 15: Sensitizers
Controls and/or modifies photochemical reaction of resist during exposure.
Determines exposure time and intensity

## Slide 16: Additives
Various added chemical to achieve desired process results, such as dyes to reduce reflection.

## Slide 17: Negative Resist
Most negative PR are polyisoprene type
Exposed PR becomes cross-linked polymer
Cross-linked polymer has higher chemical etch resistance.
Unexposed part will be dissolved in development solution.

## Slide 18: Negative Photoresist
Mask
Expose
Development
Negative Photoresist

## Slide 19: Negative Photoresist
Disadvantages
Polymer absorbs the development solvent
Poor resolution due to PR swelling
Environmental and safety issues due to the main solvents xylene.

## Slide 20: Comparison of Photoresists
- PR
Film
+ PR
Film
Substrate
Substrate

## Slide 21: Positive Photoresist
Exposed part dissolve in developer solution
Image the same that on the mask
Higher resolution
Commonly used in IC fabs

## Slide 22: Positive Photoresist
Novolac resin polymer
Acetate type solvents
Sensitizer cross-linked within the resin
Energy from the light dissociates the sensitizer and breaks down the cross-links
Resin becomes more soluble in base solution

## Slide 23: Question
Positive photoresist can achieve much higher resolution than negative photoresist, why didn’t people use it before the 1980s?
Positive photoresist is much more expensive therefore negative photoresist was used until it had to be replaced when the minimum feature size was shrunk to smaller than 3 mm.

## Slide 24: Chemically Amplified Photoresists
Deep ultraviolet (DUV), l  248 nm
Light source: excimer lasers
Light intensity is lower than I-line (365 nm) from high-pressure mercury lamp
Need different kind of photoresist

## Slide 25: Chemically Amplified Photoresists
Catalysis effect is used to increase the effective sensitivity of the photoresist
A photo-acid is created in PR when it exposes to DUV light
During PEB, head-induced acid diffusion causes amplification in a catalytic reaction
Acid removes protection groups
Exposed part will be removed by developer

## Slide 26: Chemically Amplified Photoresist
+ H
+
Heat
+ H
+
Exposed PR
Exposed PR
Before PEB
After PEB
+
Protecting Groups
Protecting Groups

## Slide 27: Requirement of Photoresist
High resolution
  Thinner PR film has higher the resolution
  Thinner PR film, the lower the etching and ion implantation resistance
High etch resistance
Good adhesion
Wider process latitude
  Higher tolerance to process condition change

## Slide 28: Photoresist Physical Properties
Photoresist must be able to withstand process conditions
  Coating, spinning, baking, developing.
  Etch resistance
  Ion implantation blocking

## Slide 29: Photoresist Performance Factor
Resolution
Adhesion
Expose rate, Sensitivity and Exposure Source
Process latitude
Pinholes
Particle and Contamination Levels
Step Coverage
Thermal Flow

## Slide 30: Resolution Capability
The smallest opening or space that can produced in a photoresist layer.
Related to particular processes including expose source and developing process.
Thinner layer has better resolution.
Etch and implantation barrier and pinhole-free require thicker layer
Positive resist has better resolution due to the smaller size of polymer.

## Slide 31: Photoresist Characteristics Summary
Parameter
Negative
Positive
Polymer
Polyisoprene
Novolac Resin
Photo-reaction
Polymerization
Photo-solubilization
Sensitizer
Provide free radicals
for polymer cross-link
Changes film
to base soluble
Additives
Dyes
Dyes

## Slide 32: Photolithography Process

## Slide 33: Basic Steps of Photolithography
Photoresist coating
Alignment and exposure
Development

## Slide 34: Basic Steps, Old Technology
Wafer clean
Dehydration bake
Spin coating primer and PR
Soft bake
Alignment and exposure
Development
Pattern inspection
Hard bake
PR coating
Development

## Slide 35: Basic Steps, Advanced Technology
Wafer clean
Pre-bake and primer coating
Photoresist spin coating
Soft bake
Alignment and exposure
Post exposure bake
Development
Hard bake
Pattern inspection
PR coating
Development
Track-stepper integrated system

## Slide 36
Figure 6.5
Hard bake
Strip PR
Etch
Previous Process
Ion Implant
Rejected
Surface preparation
PR coating
Soft bake
Alignment
& Exposure
Development
Inspection
PEB
Approved
Clean
Track system
Photo Bay
Photo cell

## Slide 37: Wafer Clean
P-Well
USG
STI
Polysilicon
Gate Oxide

## Slide 38: Pre-bake and Primer Vapor
P-Well
USG
STI
Polysilicon
Primer

## Slide 39: Photoresist Coating
P-Well
USG
STI
Polysilicon
Photoresist
Primer

## Slide 40: Soft Bake
P-Well
USG
STI
Polysilicon
Photoresist

## Slide 41: Alignment and Exposure
P-Well
USG
STI
Polysilicon
Photoresist
Gate Mask

## Slide 42: Alignment and Exposure
Gate Mask
P-Well
USG
STI
Polysilicon
Photoresist

## Slide 43: Post Exposure Bake
P-Well
USG
STI
Polysilicon
Photoresist

## Slide 44: Development
P-Well
USG
STI
Polysilicon
PR

## Slide 45: Hard Bake
P-Well
USG
STI
Polysilicon
PR

## Slide 46: Pattern Inspection
P-Well
USG
STI
Polysilicon
PR

## Slide 47: Future Trends
Smaller feature size
Higher resolution
Reducing wavelength
Phase-shift mask

## Slide 48: Optical Lithography
Optics
Light diffraction
Resolution
Depth of focus (DOF)

## Slide 49: Diffraction
Basic property of optics
Light is a wave
Wave diffracts
Diffraction affects resolution

## Slide 50: Light Diffraction Without Lens
Diffracted light
Mask
Intensity of the projected light

## Slide 51: Diffraction Reduction
Short wavelength waves have less diffraction
Optical lens can collect diffracted light and enhance the image

## Slide 52
Light Diffraction With Lens
Diffracted light collected by the lens
Strayed refracted light
Lens
Ideal light Intensity pattern
Less diffraction after focused by the lens
Mask
ro
D

## Slide 53: Numerical Aperture
NA is the ability of a lens to collect diffracted light
NA = 2 r0 / D
  r0 : radius of the lens
  D = the distance of the object from the lens
Lens with larger NA can capture higher order of diffracted light and generate sharper image.

## Slide 54: Resolution
The achievable, repeatable minimum feature size
Determined by the wavelength of the light and the numerical aperture of the system. The resolution can be expressed as

## Slide 55: Resolution
K1 is the system constant, l is the wavelength of the light, NA = 2 ro/D, is the numerical aperture
NA: capability of lens to collect diffraction light

## Slide 56: Exercise 1, K1 = 0.6
    R
G-line 436 nm 0.60 ___ m
I-line 365 nm 0.60 ___ m
DUV 248 nm 0.60 ___ m
193 nm 0.60 ___ m

## Slide 57: To Improve Resolution
Increase NA
  Larger lens, could be too expensive and unpractical
  Reduce DOF and cause fabrication difficulties
Reduce wavelength
  Need develop light source, PR and equipment
  Limitation for reducing wavelength
  UV to DUV, to EUV, and to X-Ray
Reduce K1
  Phase shift mask

## Slide 58: Wavelength and Frequency of Electromagnetic Wave
RF
MW
IR
UV
X-ray
Visible
10
4
10
6
10
8
10
10
10
12
10
14
10
16
10
18
f (Hz)
10
4
10
2
10
0
10
-2
10
-4
10
-6
10
-8
10
-10
l (meter)
g-ray
10
-12
10
20
RF: Radio frequency; MW: Microwave; IR: infrared; and UV: ultraviolet

## Slide 59: Depth of focus
The range that light is in focus and can achieve good resolution of projected image
Depth of focus can be expressed as:

## Slide 60: Depth of Focus
)
(
2
2
NA
K
DOF
l
=
2
Focus

## Slide 61
Exercise 2, K2 = 0.6
    DOF
G-line 436 nm 0.60 ___ m
I-line 365 nm 0.60 ___ m
DUV 248 nm 0.60 ___ m
193 nm 0.60 ___ m
2

## Slide 62: Depth of Focus
Smaller numerical aperture, larger DOF
  Disposable cameras with very small lenses
  Almost everything is in focus
  Bad resolution
Prefer reduce wavelength than increase NA to improve resolution
High resolution, small DOF
Focus at the middle of PR layer

## Slide 63: Focus on the Mid-Plain to Optimize the Resolution
Photoresist
Substrate
Depth of focus
Center of focus

## Slide 64
Surface Planarization Requirement
Higher resolution requires
  Shorter l
  Larger NA.
Both reduces DOF
Wafer surface must be highly planarized.
CMP is required for 0.25 mm feature patterning.

## Slide 65: I-line and DUV
Mercury i-line, 365 nm
  Commonly used in 0.35 mm lithography
DUV KrF excimer laser, 248 nm
  0.25 mm, 0.18 mm and 0.13 mm lithography
ArF excimer laser,193 nm
  Application: < 0.13 mm
F2 excimer laser 157 nm
  Still in R&D, < 0.10 mm application

## Slide 66: I-line and DUV
SiO2 strongly absorbs UV when l < 180 nm
Silica lenses and masks can’t be used
157 nm F2 laser photolithography
  Fused silica with low OH concentration, fluorine doped silica, and calcium fluoride (CaF2),
  With phase-shift mask, even 0.035 mm is possible
Further delay next generation lithography

## Slide 67: Next Generation Lithography (NGL)
Extreme UV (EUV) lithography
X-Ray lithography
Electron beam (E-beam) lithography

## Slide 68: Future Trends
1.5
1.0
0.8
0.5
0.35
0.25
0.18
0.13
0
0.2
0.4
0.6
0.8
1
1.2
1.4
1.6
84
88
90
93
95
98
01
04
Year
Feature Size (mm)
07
10
0.10
0.07
Photolithography
Next Generation Lithography
Maybe photo-lithography
14

## Slide 69: Phase Shift Mask
Quartz substrate
Chrome pattern
Pellicle
Phase shift coating
d
nf
d(nf  1) = l/2
nf : Refractive index of phase shift coating

## Slide 70: Phase Shift Mask
Quartz substrate
Chrome pattern
Pellicle
d
Phase-shifting etch
ng
d(ng  1) = l/2
ng: refractive index of the quartz substrate

## Slide 71: Phase Shift Mask Patterning

## Slide 72: Future Trends
Even shorter wavelength
  193 nm
  157 nm
    Silicate glass absorbs UV light when l < 180 nm
    CaF2 optical system
Next generation lithography (NGL)
  Extreme UV (EVU)
  Electron Beam
  X-ray (?)

## Slide 73: EUV
l = 10 to 14 nm
Higher resolution
Mirror based
Projected application ~ 2010
0.1 mm and beyond

## Slide 74: EUV Lithography
Mask
Mirror 2
Mirror 1
Wafer

## Slide 75: X-ray lithography
Similar to proximity printer
Difficult to find pure X-ray source
Challenge on mask making
Unlikely will be used in production

## Slide 76: X-ray Printing
Photoresist
Substrate
X-ray
Beryllium
Gold

## Slide 77: Optical Mask and X-ray Mask
X-ray Mask
Beryllium
Gold
Glass
Chromium
Photo Mask

## Slide 78: E-Beam
Used for making mask and reticles
Smallest geometry achieved: 0.014 mm
Direct print possible, no mask is required
  Low throughput
Scattering exposure system (SCALPEL) looks promising
  Tool development
  Reticle making
  Resist development

## Slide 79: Electron Beam Lithography System
Wafer
Blanking Plate
Lens
Lens
Lens
Electron Gun
Deflection Coils
Stigmator

## Slide 80: SCALPEL

## Slide 81: Ion Beam Lithography
Can achieve higher resolution
  Direct writing and projection resist exposing
  Direct ion implantation and ion beam sputtering patterned etch, save some process steps
Serial writing, low throughput
Unlikely will be used in the mass production
Mask and reticle repairing
IC device defect detection and repairing

## Slide 82: Safety
Chemical
Mechanical
Electrical
Radiation

## Slide 83: Chemical Safety
Wet clean
  Sulfuric acid (H2SO4): corrosive
  Hydrogen peroxide (H2O2): strong oxidizer
Xylene (solvent and developer of PR): flammable and explosive
HMDS (primer): flammable and explosive
TMAH (+PR development solution): poisonous and corrosive

## Slide 84: Chemical Safety
Mercury (Hg, UV lamp) vapor
  highly toxic;
Chlorine (Cl2, excimer laser )
  toxic and corrosive
Fluorine (F2, excimer laser)
  toxic and corrosive

## Slide 85: Mechanical Safety
Moving Parts
Hot surface
High pressure lump

## Slide 86: Electrical Safety
High voltage electric power supply
Power off
Ground static charges
Tag-out and lock-out

## Slide 87: Radiation Safety
UV light can break chemical bonds
Organic molecules have long-chain structure
More vulnerable to the UV damage
UV light can be used to kill bacteria for sterilization
Can cause eye injury if direct look at UV source
UV protection goggle sometimes is required.

## Slide 88: Summary
Photolithography: temporary patterning process
Most critical process steps in IC processing
Requirement: high resolution, low defect density
Photoresist, positive and negative
Process steps: Pre-bake and Primer coating, PR spin coating, soft bake, exposure, PEB, development, hard bake, and inspection
NGL: EUV and e-beam lithography